## Slide 1
Third JCL @ LPSC – 02 Nov 2014 Denis Grondin, Julien Giraud
Si/W ECAL Endcap structures and cooling studies @ LPSC - Grenoble –nov 2014
Design of the EM end-caps
2. Cooling system (end-caps + barrel) 3. Assembly of the EM calorimeter (ends-caps + barrel)

## Slide 2
Fastening system on HCAL: thick.3cm
185 mm
Detector slab (Si)
Moulding of one layer / 3 alveoli L = 2.490 m wall thick. = 0.5mm
R~2050
End-Caps: modular alveolar structure - composite W / Carbone HR - 25,5 t 2 x 12 independent modules - 2 x 540 alveoli
Ongoing developments 2015
- Moulding of 3 layers of 3 alveoli - 2,5m End-Cap
- Design of specific tools / long wrapping
- Optimization of deflection values / skin thickness
- Design of an assembly mould for End-cap demonstrator
I - Towards full detector – End Caps
End-Cap thick composite plate 13mm+ inserts for double row rails

## Slide 3
Chart: Degradation of structure Effort/ global displacement – 3 cycles
I.2- Composite structure: shearing tests
Charge & discharge cycles: hysteresis in specimens’ behaviour which evolves towards a progressive decrease in the force / displacement with the gradual breakdown of the resin before destruction of the composite
Impact on ECAL dead zone
CC202-ET445 sample n°4 (after CRP cycles)
Progressive load
Carbone
w
g
Problem of bending stress of alveoli skins: influence / evolution of thickness of outer plies
Chart: Effort(N)
| 1377 | 1116 | 771
 | 0.3 | 0.3 | 0.3
Sample E4, decrease of effort at constant displacement
Shearing tests stress in the structure
Dummy composite structures for plies’ thickness validation

## Slide 4
Progressive loss of stiffness for the dummy structure after each cracking level – Comparison @ constant displacement
I.3- Composite structure: shearing tests
Ongoing developments 2015
Coming next: Reduction of diameter -> modification of all modules...
Tsaï wu criteria
Adapt FEA parameters to simulate the whole structure
Safety coefficient
Static: Sufficient / to the stress induced by weight of modules
not sufficient / seism (s =3.2 for Japan?)
/ risks during integration and transport
-> increase nb of ext. plies... Impact on ECAL dead zone
Chart: Safety Coefficient Degradation / repeated stress for each module
| 67160.187969230785 | 54430.479138461531 | 37603.852523077046
M3 - E4 | 2.8 | 2.2 | 1.5
M2 - E4 | 2.8 | 2.3 | 1.6
M1 - E4 | 2.8 | 2.3 | 1.6
M3 - E3 | 3 | 2.6 | 2.6 | 2.5
M2 - E3 | 3 | 2.6 | 2.6 | 2.5
M1 - E3 | 3 | 2.6 | 2.6 | 2.5
M3 - E2 | 2.0561 | 2.1823 | 1.922 | 1.6637 | 1.2593 | 1.1192
M2 - E2 | 2.0957 | 2.2242 | 1.959 | 1.6957 | 1.2835 | 1.1407
M1 - E2 | 2.1046 | 2.2338 | 1.9673 | 1.703 | 1.289 | 1.1456
M3 - E1 | 1.6032 | 1.4611 | 1.5752 | 1.4771 | 1.4371 | 1.4371 | 1.297 | 1.299 | 1.293 | 1.243
M2 - E1 | 1.6193 | 1.4758 | 1.591 | 1.492 | 1.4515 | 1.4515 | 1.31 | 1.312 | 1.306 | 1.2554
M1 - E1 | 1.6208 | 1.4771 | 1.5925 | 1.4933 | 1.4529 | 1.4529 | 1.3112 | 1.3132 | 1.3072 | 1.2566
M2
M1
s = Cc / Cs = 2,8
S = 2,2
S = 1,5
MODULE
-Correlation of tests with FEA simulations
● Optimization of composite wrapping / long structure
● Shearing tests on demonstrator
-Ensure repeatability of process & characteristics

## Slide 5
ECAL: Optimization impact
Possible new geometry (H.Videau): Barrel: 5 modules of 3 alveoli
– LBarrel = 3829mm (Z endcap = 3929mm).
Endcaps: Quadrants of 2 modules of 2 and 3 alveoli
– with R(ECAL Ring) = 40cm + Integer number of Wafers
⇒ REndcap = 1726mm
Impact / Evolution of diameter
Infrastructure
Module‘s weight / deformation
Module‘s length / composite fab.
Cooling
Electronics in development => uncertainty on final power (4.5 KW to 30 KW)
We must move forward and propose models and tests / re-adaptation of the full leak less loop
General distribution for now:
Water circulation @ sub atmospheric pressure
Water temperature input: 18°c - Water temperature output: 23°c
Maximal power per column: 150 W
Pipes diameter : 13 mm
ECAL End-cap D=4188 | Weight(kg)
 | 25208
Module 1 | 1585
Module 2 | 2164
Module 3 | 2553

## Slide 6
Study from the power source to the global cooling II.2-1Thermal tests of the heat exchanger
II.2-2 Full scale leakless loops
cooling station
13m High Line
9 m Low Line
10 m Medium Line
2,5 m
5,1 m
4,5 m
Cooling Station
LPSC cooling test area with a drop of 13 m
II – Cooling: leakless water system
Thermal simulations / power variations (limit of pulsing)
Water heat exchanger design near detector
Ongoing developments 2015
-Full scale leakless loop Integration
-Cooling station integration+ network
Update of water heat exchanger / BGA
Thermal tests & simulations / power variations (limit of pulsing)
Cooling station
Validation of leakless system (<1atm)
EUDET adaptation of Water heat exchanger
Caloduc Prototype
Water Heat Exchanger / EUDET

## Slide 7
II.1 - Cooling: Full scale leakless loops
3D Barrel distribution
Distribution test plate
Leak less loops construction : Distribution test plate
Goal : Pressure measurement / residual bubble…….
cooling station
13m High Line
9 m Low Line
10 m Medium Line
2,5 m
5,1 m
4,5 m
Cooling Station
ECAL End-Cap Intrados: integration with cooling leak less lines
Link Tube Ti /fitting electron beam welding Ti
Titanium Fitting LAPP / ATLAS IBL
Insulator: Transition Ceramic/Titanium
Connection integration

## Slide 8
II.2 - Cooling: on going work
Cooling station assembling :
Pipe wiring => ok
Electrical wiring => to be done
Full scale leak less loops :
cooling station
13m High Line
9 m Low Line
10 m Medium Line
2,5 m
5,1 m
4,5 m
Cooling Station
Cooling station assembling
Pipe /valve / flowmeter

## Slide 9
Test of a two-phase HEATPIPE
II.3 - Cooling: Thermal tests
Study & prototype of a flat two-phase thermal diffuser (spreader)
ALICE ITS IB stave Microchannels
Water Heat exchanger preferred
EUDET adaptation of Water heat exchanger to BGA geometry - 2015
Test bench
X
X
?

## Slide 10
7 mm
Example of ALICE integration tooling
Too large / 3 cm for CALICE
< 3 cm
Guiding and fastening system of modules (ends-caps + barrel)
III - Assembly of the EM calorimeter
1 / Specific shaped rails
HCAL END-CAP
ECAL END-CAP
Ongoing developments 2015
Validation of technological solutions (bending of modules)
  Optimization / simulation of best localisation on modules
  Integration of heavy handling tool for modules’ tests / rails
2 / Self-aligning rollers
Double row sized rail on End cap thick plate
specific handling and positioning tool for integration
Construction on going