## Slide 1: The Helium-3 Removal System at the PULSTAR SOS Experiment
Christian White
15 Feb 2021

## Slide 2: Outline
What is the SOS experiment?
The 3He removal System in the SOS Apparatus
  Film Burner
  Charcoal Pump
  Gas-Gap Heat Switch
  Cryogenic Valve
Characterization of the Charcoal Adsorption Pump

## Slide 3: The Systematic and Operational Studies Apparatus at NC State/TUNL
Small scale version of SNS nEDM experiment
Cryogenic turnaround  Weeks vs months
Used to investigate systematics (geometric phase effect) and operational procedures for SNSnEDM
No Electric Field
SNS nEDM at ORNL
PULSTAR SOS at NCSU/TUNL
Notes: New pictures on review website.

## Slide 4: Schematic of the SOS Experiment
Single measurement cell (same size as SNS) full of superfluid helium
Polarized 3He (MEOP) and ultracold neutrons (NC state source) introduced into cell for measurement
After measurement, 3He flushed upward toward buffer cell and removed by a charcoal adsorption pump

## Slide 5: 3He Removal in SOS Experiment
3He can be selectively removed because of high vapor pressure
Three Main Components
  Superfluid Film Burner
  Cryogenic Isolation Valve
  Charcoal adsorption pump

## Slide 6: Design Requirements for 3He Removal
Powerful pump (charcoal adsorption) near liquid helium surface (pumping speed limited by geometry)
  Ability to cool a large amount of charcoal to 4K
  Ability to regenerated pump and remove gas when saturated
  Gas capacity for at least 1-2 weeks between regeneration

## Slide 7: Charcoal Pump Design
Brazed Copper can with top and side flange
20 copper plates
  Charcoal epoxied to one side with DP190
  Separated by spacers
Total of 0.4kg of activated charcoal
  Capacity of 5.5mols helium
  Worst case is 0.03 mols/hour – 165 hours of run time without regeneration
  Goal is to regenerate weekly
Charcoal Pump in Test Setup
Mounting Charcoal Plates
Charcoal Pump
Heat switch, linking to 4K

## Slide 8: Thermal Cycling to Regenerate Pump
Pump will operate at 4K linked to liquid He bath.
Need to raise to >25K to expel all gas when saturated
Need to heat pump without boiling off too much helium  Heat Switch
Need to isolate pump from system when regenerating  Cryogenic Isolation Valve
Isolation Valve Location
Heat Switch

## Slide 9: Gas Gap Heat Switch
Uses thermal conduction across a small gap filled (or not filled) with helium to provide (break) the thermal connection to the 4K bath
Small charcoal adsorption volume can remove helium in gap between two copper pieces
Switch is on when charcoal is warm, off when cold.
Small Charcoal Pump with Heater and Link to 4K
Heat Switch
Heat Switch in Test Setup

## Slide 10: Cryogenic Isolation Valve
100 lb. closing force
Pneumatic Actuator
Valve Seat
Valve Body
In test setup

## Slide 11: Cryogenic Isolation Valve
1cm stainless steel valve
Open during normal operation, closed during pump regeneration
Polishing + Lapping + Kapton gaskets = 10-3 to 10-2 mbar*L/s
Epoxying gasket to valve body and allowing to cure under force = 10-5 mbar L/s
Notes: Actuator Pictured

## Slide 12: Fully Assembled View
Charcoal Pump
Heat Switch
Buffer Cell
Film Burner
Valve

## Slide 13: Pumping speed. Temperature Dependence
m*= 3He quasiparticle mass =2.4m
2.8K = Binding energy of 3He to bulk LHe
C = Conductance to pump from geometry (l/s)
Estimated C ≈ 0.20 l/s
3He concentration after run ~10-10  Goal after removal ~10-12
Need at least 3-4 removal times ()

## Slide 14: Adsorption Capacity of Activated Charcoal
4He concentration 10 orders of magnitude higher, so it will dominate saturation despite higher SVP of 3He
At 10-5mbar (SVP of 4He at 0.5K), capacity of 0.4kg charcoal is ~5.5mol @4.2K

## Slide 15: Pump Adsorption Capacity Tests - Procedure
Cooled pump with cryocooler (reached 7.8K)
Filled a 100L buffer tank with 4He.
Allowed a large puff of gas into the charcoal pump
Pump will heat up as it adsorbs, when temperature reached equilibrium again, record pressure and amount of helium used.
Repeat until pump is saturated

## Slide 16: Pump Adsorption Capacity Tests - Data
4.2K and 10K curves from Salmelin shown, with interpolated 7.8K (test setup)
Data follows curve above 10-4 mbar, but below….
Trouble pumping below background of 10-5 mbar (on gauge, 10-4 when adjusted to 4He)

## Slide 17: Summary and Outlook
Helium-3 removal system complete and ready to be tested in main apparatus
Cryogenic valve are operational to leak rate of 10-5 mbar*L/s
Charcoal pump capacity behaves as expected
Entire 3He removal system has been installed in SOS apparatus; cooldown expected by early March.

## Slide 18: Thank you!

## Slide 19: Helium Film Burner