## Slide 1
New hybrid technology for thin film deposition of transparent conductive oxides -
photovoltaic applications
18/03/2023
Zakariae EN-NAJI
18/03/2024
Supervised by :
Ana LACOSTE (Thesis director, LPSC)
Alexandre BES (Co-supervisor, LPSC)
Perrine CARROY (Co-supervisor, Cea Liten)
Plasmas-Matériaux-Nanostructures team (CRMPN)

## Slide 2
Content
Context and objectives
Hybrid Plasma Deposition (HPD) technique presentation
  Plasma source
    Microwave simulation
    Plasma characterization
  Evaporation source
Deposition and characterization of Indium tungsten oxide (IWO) films
Conclusion and perspectives

## Slide 3
www.nrel.gov/pv/interactive-cell-efficiency.html
Made up of transparent conductive oxides (TCOs)
Good electrical conductivity
Low resistivity
Transparency
TCOs thin films are deposited by different techniques
Chemical Vapor Deposition
Atomic Layer Deposition
Spin Coating
Spray Pyrolysis
Cathode sputtering (magnetron)
Evolution of energy conversion efficiency over time.
.
Context and objectives

## Slide 4
The sputtering process and possible damage mechanisms.
doi.org/10.1016/j.matt.2021.09.021
Context and objectives
It is essential to suggest alternative technologies to overcome this problem
High kinetic energy of plasma particles (up to 400 eV) can damage sensitive layers of cells.
Destruction of material properties, thereby limiting or degrading cell performance.
Magnetron sputtering

## Slide 5
Context and objectives
Schematic of Reactive Plasma Deposition RPD technique
Low damage to the substrate, incident energy of ions to the substrate is in the range of 3–70 eV
High-quality of TCO films ( Resistivity, transparency, …)
Incident energy and plasma density distributions of various plasma deposition methods
doi.org/10.1186/s11671-019-2948-4
Reactive Plasma Deposition

## Slide 6
Content
Context and objectives
Hybrid Plasma Deposition (HPD) technique presentation
  Plasma source
    Microwave simulation
    Plasma characterization
  Evaporation source
Deposition and characterization of IWO films
Conclusion and perspectives

## Slide 7
Hybrid Plasma Deposition technique
TCO
Microwave injection
Head to head magnet
Solid material
DC Heater
Evaporated atoms
ECR Zone
N
S
S
N
N
S
S
N
Length (mm)
Schematic of HPD experimental setup.
Process parameters :
Pressure
Gas composition
Microwave power
Heating current
Source – substrate distance
Hybrid Plasma Deposition = Plasma source + Evaporation system

## Slide 8
Plasma source and the non-uniformity of plasma
The non-uniformity of the thin film
The need for the simulation of the microwave applicator to understand the problem
Hybrid Plasma Deposition technique

## Slide 9
Content
Context and objectives
Hybrid Plasma Deposition (HPD) presentation
  Plasma source
    Microwave simulation
    Plasma characterization
  Evaporation source
Deposition and characterization of IWO films
Conclusion and perspectives

## Slide 10
Microwave simulation: Current Microwave applicator configuration (2,45 GHz)
Principle of the 2-port model.
Geometry/material definition → Simulation using Comsol multiphysics → Data processing
 | Existing configuration
Dint | 60mm
Dext | 66 mm
Connector position (z) | 26 mm
Applicator length | 201 mm
Connecteur Dint | 10,5 mm
Connecteur Dext | 4,85 mm
Propagation medium | Air
Configuration dimensions: Existing at LPSC.
Dint connecteur
Port 1
Port 2
L
Dext connecteur
Dint
Dext
Objective of the COMSOL simulation:
Understand the source of the non-uniformity of the electromagnetic field
5,71 Ω

## Slide 11
S11 reflection as a function of frequency.
f (GHz)
Reflection of -7 dB (20%)
Ey component
Ex component
NormE
Current configuration
Port 1
Port 2
50 Ω
5,71 Ω
Microwave simulation: Current Microwave applicator configuration (2,45 GHz)

## Slide 12
TCO
Microwave injection
Head to head magnet
Solid material
DC Heater
Evaporated atoms
ECR Zone
N
S
S
N
N
S
S
N
Length (mm)
Schematic of HPD experimental setup.
Microwave simulation: Current Microwave applicator configuration (2,45 GHz)
Objective of the simulation:
Improve the geometry in order to allow microwaves to propagate in a symmetrical way
Obtain the lowest possible reflection coefficient

## Slide 13
50 Ω
5.71 Ω
24,31 Ω
135 mm
164 mm
Microwave simulation : 2-section model with a fixed inside diameter ( Frequency: 915 MHz )
 | Dint | Dext | Characteristical impedance | Length | Total length
2nd section | 60 mm | 66 mm | 5,71 Ω | 135 mm | 299 mm
1st section |  | 90 mm | 24,31 Ω | 164 mm | 
Ex component
Ex component
Model characteristics
NormE
Symmetrical EM
field
~ 100% power transmission
Symmetrical propagation of the Electromagnetic field
S11 reflection as a function of charge ( 2 ports simulation).
Reflection of -31 dB (~ 0%)

## Slide 14
50 Ω
24,31 Ω
12,31 Ω
5,71 Ω
Microwave simulation : 3-section model with a fixed outside diameter (Frequency : 915 MHz)
Ex
Ex component
 | Dint | Dext | Characteristical impedance | Length | Total length
1st section | 46 mm | 66 mm | 21,64 Ω | 144 mm | 299 mm
2nd section | 54 mm | 66 mm | 12,03 Ω | 20 mm | 
3rd section | 60 mm | 66 mm | 5,71 Ω | 135 mm | 
NormE
Symmetrical EM
field
Model characteristics
Port 2
Port 1
S11 reflection as a function of charge ( 2 ports simulation).
Reflection of -25 dB (~ 0%)
~ 100% power transmission
Symmetrical propagation of the Electromagnetic field

## Slide 15
Content
Context and objectives
Hybrid Plasma Deposition (HPD) presentation
  Plasma source
    Microwave simulation
    Plasma characterization
  Evaporation source
Deposition and characterization of IWO films
Conclusion and perspectives

## Slide 16
Ion energy distribution functions
300 W, 1 mTorr, Argon and gas mixture (84% Ar, 14% O2, 2% H2).
Energy of ions and neutral particles less than 30 eV
Plasma characterization : Ion energy distribution measurements

## Slide 17
Plasma characterization : Langmuir Probe Measurements
Langmuir Probe Measurements of Argon Plasma at 1 mTorr gas pressure
and 300W microwave Power.
(b) Plasma and floating potential
(a) Ion current density measured at various distances (11 and 16.5 cm)
Positioning of Langmuir probe.
The uniformity of ionic current and plasma distribution enhances as the source-probe distance increases
From the plasma potential and the energy of ions, we can deduce that the energy of particles involved in the process doesn’t surpass 50 eV

## Slide 18
Content
Context and objectives
Hybrid Plasma Deposition (HPD) presentation
  Plasma source
    Microwave simulation
    Plasma characterization
  Evaporation source
Deposition and characterization of IWO films
Conclusion and perspectives

## Slide 19
Evaporation source : Heating elements
Heating elements used for evaporation.
Commercial
Designed
Brittleness during handling and mounting, with limited durability under stress and temperature (3 deposition processes)
Around 300 W of power consumption for a deposition rate of 0,5A°/s
No vaporization occurs throughout the process, even at a power of 1300W.
Easily mounted
Limited durability (~ 10 processes)
Around 550 W of power consumption for a deposition rate of 0,5A°/s
Deformation of the structure after few processes
Limited durability (~ 4 processes)
Around 350 W of power for a deposition rate of 0,5 A°/s

## Slide 20
Content
Context and objectives
Hybrid Plasma Deposition (HPD) presentation
  Plasma source
    Microwave simulation
    Plasma characterization
  Evaporation source
Deposition and characterization of IWO films
Conclusion and perspectives

## Slide 21
Deposition and characterization of IWO films : Substrate holder types
25mm*25mm substrates holder for Si/ glass substrates.
150mm*150 mm substrates holder for M2 industrial size wafers.

## Slide 22
Deposition and characterization of IWO films
IWO films a) on Si (b) on glass.
84% Ar, 14% O2, and 2% H2 - 300 W - 30 min.
a)
b)
SEM images of an IWO thin film deposited on Si, (a) side view (b) top view.
a)
b)
X-ray diffraction spectrum of IWO film deposited on a Si substrate.
 | Si | Glass
Average resistance | 15,49 Ω | 13,25 Ω
Resistivity | 1,3E-04 Ω.cm | 1.15E-4 Ω.cm
Average resistance and resistivity of thin films deposited on Si and glass.
Dense, homogeneous structure ; grain size = 200 - 250 nm
Polycrystalline structure with In2O3, dominant orientation (222)
Resistivity with values required for PV application

## Slide 23
IWO Solar cell.
Cell characteristic | Values LPSC (IWO) | Values LPSC (ITO) | Ref Values. CEA (ITO)
Voltage open circuit | 744 mV | 746 mV | 746 mV
Fill factor | 82,57% | 79.4% | 82.1%
Efficiency | 23,89% | 22.88% | 23.63%
Solar cells performance.
LPSC – Hall 4
CEA's inline production for solar cells
Deposition and characterization of IWO films: Solar cell performance

## Slide 24
Conclusion
Existing configuration : 2,45 GHz - Reflection of -7 dB (20%), asymmetry of the EM field
Alternative configurations – 915 MHz – 100% power transmission, symmetrical EM field
Confirmation of the low energy (< 50 eV) of the particles involved in the deposition process
Deposition of IWO (Indium Tungsten Oxide) films with conformal properties
Perspectives
Implementation of the 915 MHz optimized configuration of the applicator and plasma performance analysis
Fine-tuning of deposition process with optimized configuration
Transposition of process to photovoltaic cells and performance evaluation
Testing new TCOS materials (SnO2, ….)
Conclusion and Perspectives