## Slide 1
1
Delayed Molecular Hydrogen Production in Portlandite Under Irradiation: Reaction Mechanisms and Consequences for the Storage of Radioactive Waste
Thibaut Herin, Stéphane Poyet, Pascal Bouniol, Sophie Le Caër
CEA/Saclay, 91191 Gif-sur-Yvette, France
sophie.le-caer@cea.fr

## Slide 2: Background to the study
Every year, France produces significant amounts of radioactive waste (60 000 m3).
  70% of electricity is generated by nuclear power
  Nuclear deterrence, naval nuclear propulsion, radiotherapy, research centers, etc.
Different sources of radioactive waste in France
In 2021, the volume of radioactive waste is estimated at 1.76 million m3
Equivalent to 3 French stadiums
Different types of radioactive waste
2
Nuclear power
60.9%
Research
26.6%
Medical
0.5%
Defense
8.7%
Other industries
3.3%

## Slide 3: Types of radioactive waste
Chart: 
 | 0.36 | 0.557 | 0.059 | 0.022 | 0.002
Very low activity (VLA)
Radioactivity: 0.0004
35.9 %
55.7 %
Low and medium activity short-lived
Radioactivity: 0.12
Long-lived low-level activity (LLL-LL)
Radioactivity: 0.01
5.9 %
Long-lived average activity (LLA)
Radioactivity: 2.7
2.2%
High activity (HA)
Radioactivity: 97.2
0.2%
Breakdown of radioactive waste by volume
Several types of radioactive waste classified by activity and lifetime
Short life (less than 300 years): surface storage
Long life (several hundred thousand years): deep disposal
3

## Slide 4: Solution chosen for LLA and HA waste
Deep geological disposal
Objective: isolate waste for several millions years
4
Cementitious materials:
  Low-cost materials
  Well-known materials
  Radiation-resistant materials
  Basic environment
Packaging of LLA waste
Concrete shell
Cemented waste
Cemented sludge and radioactive concentrates (EDF)

## Slide 5: Water in cement
The role of water
  Produce a material with rheological behavior compatible with processing
  React with cement to form cementitious hydrates (cement hydration)
  In theory:
  In practice:
Portland cement
Chart: 
 | 55 | 45
Free water
(45 %)
Chemically bound water (55 %)
Water distribution in cement paste
5

## Slide 6: Interaction of water with ionizing radiation
water
Ionizing radiation
neutron
proton
Unstable parent nucleus
Daughter nucleus
α
β
or
γ
photon
Time (s)
6
Ionizing radiation
Lousada et al, Scientific Reports, 2016

## Slide 7: The dihydrogen risk
Why is H2 potentially problematic?
  A potentially explosive gas under certain conditions
  Explosive limit of H2 in air: 4% by volume
H2 production?
!
Additional source of H2?
Packaging of LLA radioactive waste
Cementitious matrix
+
radioactive waste
Water
Free water
Chemically bound water
45 %
55 %
H2
!
H2 risk quantified
Ionizing radiation
Ionizing radiation
Need to assess the various H2 source terms
7

## Slide 8: State of the art
8
Bouniol P. J Adv Concr Technol. 2022;20(2):72-84
Systemic study by Bouniol (2022)
  Comparison of experimental H2 production (hydrated and irradiated C3S paste) and theoretical production
Study results
  Radiolysis of free (pore) water alone does not account for the H2 production observed.
  Radiolysis of solid phases must exist
Experiment
Simulation of pore water only
Time (day)

## Slide 9: Controlling the surface state of materials
adsorbed water
solid
H2
H2
Ionizing radiation
solid
H2
Ionizing radiation
Selected study configuration
Two contributions to H2
  Radiolysis of adsorbed water
  Radiolysis of the solid phase
Overestimation of H2 production from solid phases
Solid with adsorbed water
Solid with no adsorbed water
10

## Slide 10: Modeling cement paste
50 - 65 % Ca3SiO5
15 - 20 % Ca2SiO4
5 - 15 % Ca3Al2O6
5 - 10 % Ca2AlFeO5
Portlandite: Ca(OH)2
C-S-H: (CaO1.70)SiO2 (H2O)1.80
composition
Portland cement
+ water
Ca(OH)2
Nonat A. Chapter 2: Hydration of cements. In: La durabilité des bétons (2e Edition). Presses de l'Ecole Nationale des Ponts et Chaussées; 2008. p. 35.
C-S-H cement
Allen A.J., Thomas J.J., Jennings H.M. Composition and density of nanoscale calcium - silicate - hydrate in cement. Nat Mater VOL 6. 2007;6:311-6.
11

## Slide 11: Water re-adsorption kinetics
Desorption treatment
Solid particle
Adsorbed water
Solid particle
12

## Slide 12: Water re-adsorption kinetics
Desorption treatment
Air exposure
Solid particle
Adsorbed water
Solid particle
Solid particle
Adsorbed water
Measurement of water re-adsorption kinetics
  Use of vapor sorption dynamics (VSD)
  Exposure of samples to a range of relative humidity 0-60%.
  Measuring mass change
13

## Slide 13: Measurement of H2
Tightly-closed valve
powder
1.6 bar
argon
Ampoule
in glass
Sample preparation
  Minerals in powder form
  Desorption and irradiation treatment in the same ampoule
  Possibility of sampling ampoule atmosphere after irradiation
  Measurement of H2 production by gas-phase micro-chromatography (µ-GC)
14
Sample storage in glove box
with ultra-pure argon & H2O content < 0.5 ppm

## Slide 14: The ALIENOR linear electron accelerator
10 MeV electrons
Pulse duration: 10 ns
Repetition frequency: 1-10 Hz
Dose: 20 Gy/pulse
Dose rate: 2 1010 Gy/s
Ampoule positioning
10 ns
10 ns
10 ns
time
dose
15
Irradiation with Jorge VIEIRA

## Slide 15: Removal of adsorbed water from portlandite
Using radiolysis to check for the presence of adsorbed water
Desorption plateau
(stable H2 production)
Heat treatment intensity
Production of H2
Unaltered mineral with no adsorbed water
Mineral containing adsorbed water
Solid radiolysis + adsorbed water
(high production of H2)
Probable
Mineral alteration and removal of chemically bound water
Unlikely
Altered mineral
Ca(OH)2 particle
Adsorbed water
H2
H2
Ca(OH)2 particle
H2
Ca(OH)2 particle
H2
16

## Slide 16: Removal of adsorbed water from portlandite
Time/temperature mapping
Desorption treatment
  Water removal by heat treatment under primary vacuum (0.1 - 1 mbar)
  Treatment of increasing intensity
  Measuring H2 radiolytic yield
Temperature Time | 120°C G(H2) (mol.J-1) 109 | 150°C G(H2) (mol.J-1) 109 | 180°C G(H2) (mol.J-1) 109 | 200°C G(H2) (mol.J-1) 109
6 h | 6.8 ± 0.7 | 5.4 ± 0.5 | 3.9 ± 0.4 | 3.0 ± 0.3
16 h | 4.9 ± 0.5 | 4.8 ± 0.5 | 3.5 ± 0.4 | 3.6 ± 0.4
64 h | 5.5 ± 0.5 | 3.6 ± 0.4 | 3.0 ± 0.4 | 3.4 ± 0.4
17
Herin et al., Rad. Phys. Chem., 243, 113715 (2026)

## Slide 17: Delayed production of H2 in portlandite
Ca(OH)2 samples
Ionizing radiation
Immediate H2 production
Delayed H2 production
Gradual release
Directly accessible
Delayed production of H2
  Similar phenomenon demonstrated on aluminum oxy(hydroxides) by Kaddissy (2016)
  H2 not directly accessible
  Delayed production increases with the initial dose delivered
After initial irradiation, portlandite progressively releases H2
18
Herin et al., J. Phys. Chem. C, 127, 20245 (2023)

## Slide 18: Influence of temperature on delayed H2
Delayed production is heat-activated
  Irradiation at 400 kGy and delayed production monitoring for several temperatures
  Convergence at temperatures above 100°C
19
Type of H2 considered | G(H2) (mol.J-1)
Immediate | 3.0 10-9
Immediate + delayed | 1.2 10-8
Time (days)
Time (days)
Herin et al., J. Phys. Chem. C, 127, 20245 (2023)

## Slide 19: Origin of delayed H2
Good correlation with μ-GC measurements
1H NMR analysis of irradiated portlandite samples
  Appearance of a signal at 4.3 ppm in irradiated samples (trapped H2)
  Tracking the intensity of the 4.3 ppm peak with temperature
20
In collaboration with Thibault Charpentier (CEA Saclay/NIMBE/LSDRM)
Herin et al., J. Phys. Chem. C, 127, 20245 (2023)

## Slide 20: Electron paramagnetic resonance analysis of Ca(OH)2
Zoom
Electron paramagnetic resonance (EPR) spectroscopy
  Method for detecting radical (paramagnetic) species formed during irradiation
  Irradiation of Ca(OH)2 samples in liquid nitrogen at 20 kGy and EPR detection at -150°C
Presence of paramagnetic species: (in the volume), (on the surface) and
21
In collaboration with Antonino Alessi (CEA Saclay/LSI)
Herin et al., J. Phys. Chem. C, 128, 19529 (2024)

## Slide 21: Mechanism of H2 production in portlandite
  Ionic mechanism
  Excitonic mechanism
Equality never observed in practice
or
The presence of is an argument in favour of radiolysis of CaO-H bonds
Primary event
22
Herin et al., J. Phys. Chem. C, 128, 19529 (2024)

## Slide 22: Mechanisms of H2 production in portlandite
Ca(OH)2
H2 (total)
Immediate H2
Ionic (and excitonic) mechanism
Delayed H2
Volume  surface transport
Surface
Volume
Recycling
23
Herin et al., J. Phys. Chem. C, 128, 19529 (2024)

## Slide 23: Simulation of delayed H2 production after irradiation of portlandite
  Spherical particles
  Isotropic diffusion with radial geometry
  Fickian diffusion
  Homogeneous initial concentration
Diffusion model assumptions
Equations of the diffusion model
  Poor model convergence at low temperatures
  At least one of the hypotheses is false
Problems
27
Time (h)

## Slide 24: Sub-diffusion modeling
H2 transport in portlandite is a sub-diffusive process
Evidenced by Honorio de Faria and Trifa using molecular dynamics calculations
Subdiffusion model equations
: Fickian diffusion
and : subdiffusion
28
Honorio et al., J. Phys. Chem. C, 128, 19085 (2024)
Time (h)
experiments

## Slide 25: Using a more "realistic" portlandite
In cement, portlandite crystals are micrometric (1 to 100 μm).
  Typical size: 100 nm
  Specific surface area: 25 m².g-1
Ca(OH)2 (standard)
  Typical size: 1-2 μm
  Specific surface area: 2 m².g-1
Ca(OH)2 (recrystallized)
Thermal cycling in a hydrothermal reactor
29
Simulation of the H2 concentration profile in portlandite particles
R = 50 nm
R = 1000 nm
H2 concentration (a.u.)
Immediate H2
Delayed H2

## Slide 26: Conclusions
Study assumptions
  Cement can be assimilated to tricalcium silicate (Ca3SiO5)
30
   The total absence of adsorbed water is necessary to study the radiolysis of bound water without any parasitic contribution.
   The notion of radiolytic yield can be rather tricky in the case of a solid.
    Production delayed over several days (and specific surface area effects....)
   The immediate production of H2 is due to surface phenomena.
   The delayed production of H2 is due to dihydrogen molecules trapped in the crystalline structure, which diffuse slowly towards the surface via sub-diffusion.
   EPR spectroscopy can be used to propose reaction mechanisms for irradiated portlandite by identifying radiation-induced defects.
   High H2 retention capacity for micrometric particles

## Slide 27
  Thank you for your attention

## Slide 28: Influence of portlandite purity
Irradiation of high-purity portlandite
  Disappearance of dose offset
  Higher H2 production
32
EPR analysis of standard portlandite
  Irradiation at 20 kGy at room temperature
  Decrease in Cr3+ and Mn2+ with irradiation
Ca(OH)2 pure | Ca(OH)2 ultrapure
CaO (99.95% purity) | CaO (99.998% purity)

## Slide 29: State of the art
Radiolytic yield:
Reference yields:
Δn(Xi): quantity produced/destroyed (mol)
Dose: Gray (J.kg-1)
m: irradiated mass (kg)
9
Author | Treatment prior to irradiation | G(H2) (mol.J-1)  108
Yin et al (2019) | *R.H. = 30%. | 3.6
 | Lyophilization | 3.3
Le Caër et al. (2017) | T = 110°C + R.H. = 11% | 1.3 – 2.3
 | T = 110°C + R.H. = 0% (0°C) | 0.3 – 0.5
Ishikawa et al (2019) | T = 40°C | 1.4
 | T = 120°C | 0.06
* Relative humidity
Measuring radiolytic yields on cement paste
Irradiation with free water
Attempt to remove adsorbed water

## Slide 30: Extrapolation to a real material
Portlandite: Ca(OH)2
Laboratory materials
Radiolysis of solid phase and production of H2
Proposition of production mechanisms
Portlandite stores some of the H2 produced
Results
Laboratory results are difficult to transpose to an operational context
  Use of an irradiation source with a more realistic dose rate
  How much H2 should be counted for portlandite?
  Is the portlandite used representative of the portlandite in a cementitious matrix?
ALIENOR Accelerator
24

## Slide 31: Influence of dose rate
ALIENOR Accelerator
1013 Gy.h-1
Operating context
Laboratory
Gamma source 137Cs
270 Gy.h-1
Ca(OH)2
Radioactive waste packages
t0 Gy.h-1
25
Molecular hydrogen production follows the same trend regardless of whether the irradiation is done with gamma rays or accelerated electrons;
The H2 radiolytic yield is 2 to 3 times higher with gamma irradiation, despite its dose rate being several orders of magnitude lower than that of electron irradiation.
« Immediate » H2 production

## Slide 32: How much H2 should be considered in portlandite? Can we model H2 transport?
Modeling delayed H2 transport
Determination of portlandite particle size
  Observation by TEM (Transmission Electron Microscopy)
  Image analysis to obtain particle size distribution
26
Processing
Radius of the particles (nm)
Number of detected particles