## Slide 1: R&D at CERN for superconducting radiofrequency cavities

## Slide 2: Motivation
Power consumption in a superconducting cavity is proportional to its surface resistance RS
RS shows a complex behavior on external parameters, such as temperature, frequency, magnetic and electric field
Some open questions:
  Origin of the residual resistance
  Origin of the field-dependent resistance
  Stronger field-dependent resistance of niobium films compared to bulk niobium
  Influence of magnetic and electric field
  Relation to the surface properties
  Possibilities and limitations of materials other than niobium

## Slide 3: Motivation
PhD Project 1 - Sarah Aull (Univ. Siegen):
RF characterization of samples over a wide parameter range using a Quadrupole Resonator to test surface resistance models on different materials
PhD Project 2 - Giovanni Terenziani (Univ. Sheffield):
Develop High Power Impulse Magnetron Sputtering (HIPIMS) coatings to overcome limitations of standard Direct Current Magnetron Sputtering (DCMS) coatings

## Slide 4
150 liter lHe cryostat
Concrete bunker
X-ray detector connected to interlock system
Insert with Quadrupole Resonator
200 W RF system 400-1500 MHz
Helium Dewar
Manostat

## Slide 5: Design of the Quadrupole Resonator
361 mm
Sample diameter: 75 mm
The sample needs to be EB-welded to the sample cylinder
Bulk niobium and copper samples are available
Niobium Sample
Copper Sample
Niobium Cylinder
Stainless Steel Flange

## Slide 6: Field Configuration & Features
Resonant frequencies:
400, 800, 1200 MHz
Almost identical magnetic field configuration
Ratio between peak magnetic and electric field proportional to frequency
B׀׀
0
max
50 mm

## Slide 7: The Calorimetric Technique
Niobium
Rods
Quadrupole Resonator
Sample Surface

## Slide 8: The Calorimetric Technique
DC Heater
Quadrupole Resonator
Thermometry Chamber
Heat Flow
Measuring the temperature on the sample surface
Precise Calorimetric measurements over wide temperature range
Temperature
Sensors
Sample Surface

## Slide 9: The Calorimetric Technique
time
Temperature
Bath
Temperature
Temperature
of Interest
PDC,1
PDC,2
PRF
Power
DC on
RF on
≈60 s
≈40 s
Temperature
Sensors
DC Heater
Heat Flow

## Slide 10: The Calorimetric Technique
time
Temperature
Bath
Temperature
Temperature
of Interest
PDC,1
PDC,2
PRF
Power
DC on
RF on
≈60 s
≈40 s
Temperature
Sensors
DC Heater
Heat Flow
Measured directly
Measurement of transmitted power Pt
Pt=c∫H2ds, c from computer code

## Slide 11: Flux Trapping

## Slide 12: Flux Trapping
Sample
DC Coil

## Slide 13: Flux Trapping
DC Coil

## Slide 14: Trapped Flux at 400MHz and 4K
Bulk niobium sample
Reactor grade, RRR
Standard BCP, no bake out

## Slide 15: Magnesiumdiboride MgB2
Material | Bulk Niobium | MgB2
Rres | A few nΩ | ?
dR/dT (theoretically well understood) | Lowest for all elements | Better
dR/dB | Lowest increase, best studied material | So far worse, very few measurements
Bc1 | Close to Bc ≈ 200 mT | Worse
Bsh | Above Bc | Better
B. Xiao et al. - Supercond. Sci. Technol. 25 (2012)
7.5 GHz
Only magnetic field

## Slide 16: Magnesiumdiboride MgB2
Barrier in transmitted power above 1.3 mT
Multipacting?
f=400 MHz
B=1 mT
B
t

## Slide 17: Quadrupole Resonator - Summary and Outlook
Sample tests over a parameter range inaccessible to elliptical cavities:
  Three different RF frequencies, with almost identical magnetic field configuration
  Frequency dependent electric field configuration
  Wide temperature range
  Accuracy of about 0.05 nΩ
  Study the influence of trapped magnetic flux
  Unique possibilities to test surface resistance models and study new materials
Next sample to be tested: Niobium on Copper deposited by HIPIMS technology

## Slide 18: Lessons learned with sputtered films
288 Nb/Cu cavities installed in LEP
16 Nb/Cu cavities installed in LHC
About 300 coatings on 1.5 GHz for R&D
Low-beta studies, several 10’s of coatings
Advantages of films
  Lower losses at 4.2 K and moderate accelerating gradient compared to bulk niobium
  Reduced sensitivity to earth magnetic field, x100 less than bulk Nb: no need for magnetic shielding
  Cheaper material
Major disadvantage of films
  Steep RS increase with RF field

## Slide 19: From dcms to HIPIMS
By applying pulses of high power the sputtered target material
atoms are ionized and applying biasing potential we can achieve:
target material ions can be accelerated towards the substrate, higher kinetic energy upon arrival
ions are directed to the surface, thus non-flat surfaces can be sputtered with good uniformity of the film
dcms
352 MHz
4 K

## Slide 20: Reproducing old dcms results
Chart: Eacc in MV/m
| 2.4088745641423075 | 2.8794807918988914 | 3.4143983339813309 | 4.0300848119330519 | 4.6645976143974757 | 5.5057208212851698 | 5.892698023133204 | 6.2490526802309292 | 6.5435614597437946 | 6.8598431521851078 | 7.1996964421183582 | 7.4441340630671409 | 7.7057370630948272 | 7.9490309115279061 | 8.2378558053083974 | 8.3332456798056072 | 8.9086969537573193 | 9.5458407704624229 | 9.9957223858993984
2.26 K | 1.3142e-07 | 1.4112e-07 | 1.5303e-07 | 1.6682e-07 | 1.8704e-07 | 2.0306e-07 | 2.1586e-07 | 2.3136e-07 | 2.5259e-07 | 2.726e-07 | 2.9474e-07 | 3.2262e-07 | 3.5021e-07 | 3.8057e-07 | 4.073e-07 | 4.4942e-07 | 5.168e-07 | 6.3741e-07 | 7.6871e-07
2.1 K | 1.1238e-07 | 1.2424e-07 | 1.3404e-07 | 1.4941e-07 | 1.5749e-07 | 1.7598e-07 | 1.9783e-07 | 2.2652e-07 | 2.6992e-07 | 3.2255e-07 | 3.866e-07 | 4.6289e-07 | 5.5438e-07 | 6.22e-07 | 6.9319e-07 | 8.3254e-07 | 9.76e-07 | 1.0959e-06
1.6 K | 1.2087e-07 | 1.1839e-07 | 1.1428e-07 | 1.3142e-07 | 1.4267e-07 | 1.5885e-07 | 1.899e-07 | 2.183e-07 | 2.5422e-07 | 2.9941e-07 | 3.5815e-07 | 4.3684e-07 | 5.2734e-07 | 6.4734e-07 | 8.0369e-07 | 9.4863e-07 | 1.1627e-06
4.2 K | 6.0936e-07 | 6.2814e-07 | 6.6733e-07 | 6.7107e-07 | 7.3372e-07 | 7.6873e-07 | 7.4773e-07 | 8.3023e-07 | 8.8483e-07 | 9.2614e-07 | 9.7402e-07 | 1.0055e-06 | 1.0951e-06 | 1.136e-06 | 1.1907e-06 | 1.2364e-06 | 1.2773e-06 | 1.328e-06 | 4.2077e-07 | 5.7639e-07 | 5.7757e-07 | 5.8483e-07 | 5.9002e-07 | 5.9482e-07 | 6.021e-07 | 6.0516e-07 | 6.0821e-07 | 6.4045e-07 | 6.4764e-07 | 6.944e-07 | 7.0695e-07
dcms
1.5 GHz
No field emission up to 11 MV/m, but residual resistance of 100 nΩ and strong Q-slope

## Slide 21: Reproducing old dcms results
RS of copper at 1.5 GHz is about 1 mΩ
Rres=100 nΩ
?
Total Surface Area=670 cm2
 Uncoated surface area=6.7 mm2
Should be detectable with optical inspection system
Is the residual resistance caused by uncoated areas?

## Slide 22: Optical Inspection

## Slide 23: Optical Inspection
≈1 mm

## Slide 24: Acknowledgement
Quadrupole Resonator: S. Aull, S. Doebert, J. Knobloch
Coating of cavities: G. Terenziani, S. Calatroni, A. P. Ehiasarian
Optical Inspection: Janic Chambrillon
After 50 years of experience with superconducting cavities, we are approaching the fundamental limitations of niobium by recipes for which the underlying physics is not completely understood. For some accelerator applications SRF technology is the only choice. For reliable production, building compacter machines and cheaper electricity bills basic R&D and material studies are necessary!